# WPS-SMAW-017 - Welding Procedure Specification

SAMPLE DOCUMENT FOR TESTING ONLY. Fictional company and values; not a qualified procedure.

Scope: single-V butt welds in structural steel plate for general fabrication, supported by PQR-017. Welders must hold a current qualification for the positions listed.

## Table 1: Procedure variables

| Welding process | SMAW (manual metal arc) |
| --- | --- |
| Joint design | Single-V butt, 60 degree included angle, 2 mm root gap, 1.5 mm root face |
| Base metal | IS 2062 E250 BR |
| Thickness range qualified | 10 mm to 25 mm |
| Filler metal | AWS A5.1 E7018, 3.15 mm and 4.0 mm |
| Positions | 1G (PA) and 2G (PC) |
| Minimum preheat | 50 C |
| Maximum interpass temperature | 250 C |
| Post-weld heat treatment | None |
| Electrode baking | 300 to 350 C for 2 hours, then held at 100 to 150 C in a holding oven |

## Table 2: Welding parameters

| Pass | Electrode (mm) | Current (A) | Voltage (V) | Travel speed (mm/min) |
| --- | --- | --- | --- | --- |
| Root | 3.15 | 90-110 | 21-23 | 80-100 |
| Fill | 4.0 | 140-170 | 22-25 | 120-160 |
| Cap | 4.0 | 140-165 | 22-24 | 130-170 |

## Inspection

All welds receive 100 percent visual inspection. The root pass is back-gouged to sound metal before the second-side weld. Arc strikes outside the weld groove are not permitted.